## Slide 1: Capstone Project
Thermal Insulator from Buffing Dust
Group :11
ID : 2011049-2011054

## Slide 2
Overview:
We aim to make a thermal insulator from buffing dust which mainly aims to recycle approximately 1.18 × 104 –3.54 × 104 tonne waste generated in tannery industries

## Slide 3: Materials :
Buffing Dust
Polystyrene
Blowing Agent

## Slide 4: Materials & Their Costing:
Buffing Dust
Collected from Tanneries
Polystyrene
200 tk/kg
650 tk/500 gm
Citric Acid

## Slide 5: Attempt one:
Material Ratio
Polystyrene : Buffing Dust
77 : 23

## Slide 6: Attempt one:
Result:
Brittle Material
Clear Sound Upon Cracking
Apparently hard

## Slide 7: Attempt TWO:
Material Ratio
Polystyrene : Buffing Dust : Citric Acid
77 : 20 : 3

## Slide 8: Attempt Two:
Result:
Less Hard
More foamy
Clear sound upon cracking

## Slide 10: Current Problem:
Absence of High to low pressure transition

## Slide 11: Requirements:
A Mould from Stainless Steel

## Slide 12: Requirements:
Access to electric arc furnace

## Slide 13: Requirements:
High Pressure co2 gas

## Slide 14: Thank you